**ANNEX 6**

**Draft Amendment No. 2 to IS 15477 : 2019 Adhesives For Use With Ceramic, Mosaic And Stone Tiles Specification (First Revision)**

|  |
| --- |
| **A-6 CONDITIONING**b) *Wet condition —* *i)* Condition the specimensunder standard conditions for 7 days.ii) Thereafter immerse in water at standardtemperature for 20 days.iii) Remove the specimens from water, wipe with a cloth,and bond the pull head plates to the tile or stone. iv) Keep the bonded sample for 7 h under standardconditions.v) Immerse the specimen in water for another day at standard temperature.vi) On the following day, after total 28 days, remove the specimens from water, wipe with a wet cloth and immediately determine the tensile adhesion strength of the adhesive as per the procedure given in |