Doc No.: CHD 19 (25481) F

**AMENDMENT NO. 2 OCTOBER 2024 TO**

**IS 12254: 2021 POLYVINYL CHLORIDE PVC INDUSTRIAL BOOTS — SPECIFICATION**

**(*Second Revision*)**

(*Page* 5, *clause* **5.5.5**, *first para, line 4)* — Substitute ‘clause **5.5** of ISO 4643’ *for* ‘Annex B of ISO 4643’.

[*Page* 6, *clause* **5.11.1**, *third para* (*see also Amendment no. 1*)] — Substitute the following for the existing:

When tested in accordance with IS 15298(Part 1), the sole thickness shall be as under:

1. Forepart

d1: 6 mm, *Min*

d2: 4 mm, *Min*

1. Heel

d1: 9 mm, *Min* d2: 6 mm, *Min*