# Doc TED 06 (24775) F

# AMENDMENT NO. 5 AUGUST 2024

# TO

**IS 2553 (PART 2): 2019 SAFETY GLASS — SPECIFICATION PART 2 FOR ROAD TRANSPORT**

(*First Revision*)

(*Page* 2, *Clause* **3.7**) *—* Insert the following note after clause **3.7**.

‘NOTE — Wedged type glazing having variable thickness forms part of this standard. In such cases manufacturer must declare the design range of thickness and must ensure that thickness of glazing lies within the tolerance of ± (n x 0.2 mm), where n equals the number of glass layers in the glazing.’

(TED 06)