**AMENDMENT NO. 3 OCTOBER 2022**

**TO**

# IS 15961: 2012 HOT DIP ALUMINIUM — ZINC ALLOY METALLIC COATED STEEL STRIP AND SHEET (PLAIN)

(*Page* 3**,** *Table* 2) — Substitute the following for the existing:

NOTES

1. As per the mutual agreement between the customer and supplier, the steel strip and sheet with minimum coating mass other than the specified above may be supplied for each coating class. In such cases, the agreed minimum coating mass shall not be less than the minimum coating mass specified for each of the above coating classes.
2. However, in any case, the agreed minimum coating mass shall not be less than that of AZ 70.

(MTD 04) \_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_

 Publication Unit, BIS, New Delhi, India