## Slide 1: TECHNOLOGY OF ELASTOMERS
LESSON PLAN
PREPARED by
VISHANT RAWAT

## Slide 2: CURRICULUM ACADEMIA
ELASTOMERS , TYPES , CLASSIFICATION
PROPERTIES AND USES OF ELASTOMER
PROCESSING OF PLASTICS i.e Compression moulding and Injection moulding.
VULCANIZATION

## Slide 3: DEFINATION OF ELASTOMERS
An elastomer is a type of polymer with property of elasticity , generally having low Young’s Modulus and high Yield strain compared with other materials. They are known for their flexibility and resilence. They can withstand repeated stretching and compressing without losing their shape which make them ideal where rubber like material is required.
Elastomer is a very big term , all it means is rubber. Some polymers which are elastomers include polyisoprene or natural rubber, polybutadiene, polyisobutylene and polyurethanes.

## Slide 4: TYPES OF ELASTOMERS
Elastomers are categorized into
Saturated Elastomer lacks double bond in their polymer chains, excel in stability and resistance to degradation. For e.g Silicon rubber which has exceptional thermal stability, electrical insulation & biocompatibility. They cannot be treated with Vulcanisation.
Unsaturated Elastomer characterized by double bonds in their polymer chains offers exceptional elasticity and resilience. For e.g Natural rubber derived from the latex of rubber tree is iconic unsaturated elastomers. They can be trated with Vulcanisation.
UNSATURATED ELASTOMERS
SATURATED ELASTOMERS

## Slide 5
TYPES OF ELASTOMERS
GENERAL – PURPOSE ELASTOMERS SPECIALITY ELASTOMERS THERMOPLASTIC (TPE) ELASTOMERS
General purpose Elastomers includes: Specialty Elastomers includes i) TPA i. STYRENE- BUTADIENE RUBBER (SBR) i. NITRILE RUBBER (NBR) ii) TPU
ii. POLY BUTADIENE RUBBER (BR) ii. BUTYL RUBBER (IIR) iii) TPO iii. POLYISOPRENE (PIR) iii. SILICONE RUBBER iv) TPV iv. NATURAL RUBBER (NR) iv. FLUOROCARBONS RUBBERS v. SYNTHETIC RUBBER (SR) v. URETHANE RUBBERS (UR)

## Slide 6: THERMOPLASTIC ELASTOMERS (TPE)
As per the IS 17138:2019 thermoplastic elastomer is defined as polymer or blend of polymer that has properties at its service temperature similar to those of vulcanized rubber but can be processed and reprocessed at elevated temperature like thermoplastic. Thermoplastic rubber is a commonly used term for thermoplastic elastomer.
Clause 5.0 of IS 17138:2019 defines different categories of THERMOPLASTIC ELASTOMER which includes
TPA – Polyamide thermoplastic elastomer, comprising a block polymer of alternating hard and soft segments with amide chemical linkages in the hard blocks and ether/ester linkages in the soft blocks.
TPC- Copolyester thermoplastic elastomer , consisting of a block copolymer of alternating hard segments and soft segments, the chemical linkages in the main chain being ester/ether.
TPO- Olefin thermoplastic elastomer , consisting of a blend of a polyolefin and a conventional rubber, the rubber phase in the blend having little or no crosslinking.

## Slide 7: CLASSIFICATION OF TPE AS PER IS 17138:2019
TPS- Styrenic Thermoplastic Elastomer, consisting of at least a triblock copolymer of styrene and specific diene, where the two end blocks are polystyrene and internal block is a polydiene.
TPU- Urethane Thermoplastic Elastomer consisting of a block copolymer of alternating hard and soft segments with urethanes chemical linkages in the hard blocks and ether or carbonate linkages in the soft blocks. USES : Protective casing, medical equipment , in line skate wheels.
TPV -Thermoplastic rubber vulcanizate, consisting of a blend of a thermoplastic material and a conventional rubber in which the rubber has been crosslinked by the process of dynamic vulcanization during the blending and mixing step. USES : Automotive interior, dash , bumpers, roofing.

## Slide 8
Relevant
Indian
Standard

## Slide 9: WHY ELASTOMERS
HIGH ENERGY DENSITY
Capable of storing large amounts of energy with small area and volume. They can easily be stretched and rapidly recover their original dimension when applied stress is released.
The elasticity is derived from the ability of long chain to reconfigure themselves to distribute an applied stress.
LOW STRAINS
- Stress /strain profile suitable for low power electrostatic actuators with large displacements.

## Slide 10: (A) is an unstressed polymer; (B) is the same polymer under stress. When the stress is removed, it will return to the A configuration. (The dots represent cross-links)

## Slide 11: CROSS LINKING
Cross linking means that different chains of polymers molecules have all been linked
When polymer chains are crosslinked, the material becomes more rigid. The mechanical properties of a polymer depend strongly on the cross-link density.

## Slide 12: PROPERTIES OF ELASTOMERS
Hardness : It indicates an elastomer’s resistance to indentation or deformation under applied pressure. Elastomer with higher hardness value exhibit greater resistance to compression. For e.g Polyurethane find use in load bearing component where rigidity and durability are paramount.
Elongation at break : It is measure of materials ability to stretch before rupture. It reflects flexibility and resilience. Elastomers with high elongation at break values can under go deformation without failure. Natural rubber and synthetic elastomer like polyurethane exhibit impressive elongation at break.
Abrasion Resistance: It’s is measure of elastomer ability to withstand surface wear and erosion caused by frictional forces. The polymer’s molecular structure , filler content and surface finish influence its abrasion resistance. For e.g Nitrile rubber is renowed for its excellent abrasion resistance.
Tear Resistance: Tear resistance evaluates the materials resistance to tearing or propagation of cracks under applied stress. Elastomer like Ethylene- propylene – diene- monomer (EPDM) and neoprene demonstrate superior tear resistance making them indispensable in cable insulation and roofing membrane.

## Slide 13: PROPERTIES OF ELASTOMERS
Thermal Properties: Heat resistance is crucial in determining an elastomer performance at elevated temperature. Silicone elastomer renowned for their exceptional thermal stability can withstand temperature from – 60 C to 200 C without losing mechanical properties.
Chemical Resistance : Chemical resistance is another critical property of elastomers, ensuring their resilience in various acids and solvents. Nitrile rubber known for its excellent oil and fuel resistance finds widespread use in Automotive seals, gaskets. Fluorocarbon Elastomers resist a broad spectrum of chemicals, including acid , bases, and organic solvent.

## Slide 14: STRETCHING :
Elastomers can be stretched to many times their original length.
BOUNCING:
Elastomers can return back into their original shape without permanent deformation.

## Slide 15: VULCANIZATION
Vulcanization is a chemical process for converting rubber or related polymers into more durable materials via addition of Sulphur or other equivalent curatives. Charles Good year discovered the process of vulcanization.

## Slide 16: VULCANIZATION

## Slide 17: RELATED INDIAN STANDARD3400 (Part 1):2021

## Slide 18: EFFECTS OF VULCANIZATION ON RUBBER
IS 3400 Part 1: 2021 deals with the Method of test of Vulcanized rubber. The test method defines to determine the property of tensile strength, elongation at break, elongation at yield, stress at yield.
Vulcanization causes mechanical property changes such as Tensile Strength, Tear Strength, Elastic recovery.
Hysteresis reduced with increased cross – link formation. Vulcanization process cross links polymer chains, enhances tear resistance by creating network of molecular bonds. Hysteresis is the amount of plastic stretch that does not recover to final state. It is a measure of deformation energy which is not stored but converted to heat.

## Slide 19: NATURAL RUBBER
Natural rubber is a natural polymer.
Latex is a milk liquid that flows out after the bark of the rubber tree us cut. Latex is a mixture of rubber particles and water.
Natural rubber is also known as cis-1,4 –poly (isoprene)

## Slide 20: NATURAL RUBBER PRODUCTION PROCESS

## Slide 21: RELATED INDIAN STANDARD IS 5599:1999

## Slide 22: PROPERTIES OF NATURAL RUBBER
High Tensile and Tear strength
Resistance to wear , abrasion and fatigue.
High molecular weight
Rubber is water repellent.
It shows resistance against alkalies and weak acids.

## Slide 23: POLY- BUTADIENE RUBBER (BR)
Butadiene (CH2=CH-CH=CH2) is a reactive colorless gas produced by the dehydrogenation of butene or butane or by cracking of petroleum.
Polybutadiene (BR) is the second largest volume of synthetic rubber produced next to styrene – butadiene rubber. It is an important synthetic elastomer based on high content cis-1,4 polybutadiene and carbon backbone.
The polymer is noted for its high resistance to abrasion, low heat buildup, and resistance to cracking.

## Slide 24: PROPERTIES AND APPLICATION OF BUTADIENE
Good Abrasion resistance.
Elasticity and cold properties.
Low cost
Widely used in tyres because of good abrasion resistance.
Polybutadiene also has major application as an impact modifier for polystyrene and acrylonitrile – butadiene resin (ABS). IS 10016 (Part 6) : 2000 describes method of test for polybutadiene rubber.
The standard prescribes standard materials, equipment and processing methods for evaluating vulcanization characteristics of solution-polymerized ~butadiene rubbers (BR), including oil-extended types (OEBR).

## Slide 25: STYRENE BUTADIENE RUBBER
SBR belongs to the family of synthetic rubber and is derived from two monomers , Styrene and butadiene. The mixture of these two monomer are polymerized by two basically different processes: from solution (S-SBR) or as an emulsion (E- SBR).
The material was initially marketed with the name Buna S where Bu stands for Butadiene and Na for Sodium and S for Styrene.
Indian Standard available on Styrene Butadiene Rubber is given below
IS 11356 Part 1: 2023 ----- Styrene Butadiene Rubber Latex Non carboxylated.
IS 11356 Part 2: 2023 ------ Styrene Butadiene Rubber Latex Carboxylated.

## Slide 26: SCOPE OF BIS STANDARDS ON SBR
IS 11356 (Part 1) :2023 defines the requirement and methods of sampling and test for hot and cold polymerized non carboxylated styrene butadiene copolymer latex, emulsified with rosin acid and fatty acid soap emulsifier.
IS 11356 (Part 2):2023 defines the requirement and methods of sampling and test for hot and cold polymerized carboxylated styrene butadiene copolymer latex, emulsified with synthetic emulsifier.

## Slide 28: SBR (Styrene Butadiene Rubber)
PROPERTIES :
Good Abrasion and ageing properties when protected by additives.
Good heat and oil resistance.
USES:
Foot wear
Adhesive
Floor tiles
Rubber goods
Fire fighting hoses

## Slide 29: ETHYLENE – VINYL ACETATE (EVA)
It is commonly known as EVA
It is a copolymer of ethylene and vinyl acetate. Copolymers containing 50 % vinyl acetate are classified as thermoplastics.
EVA co polymer is an inert material and offers good flexibility and toughness even at low temperature , low sealing temperature , excellent stress crack resistance . [ Extracted from the foreword of Indian Standard IS 13601: 1993]
The material has good clarity and gloss, low temperature toughness, stress crack resistance, hot-melt adhesive water proof properties and resistance to UV radiation.
Ethylene –vinyl acetate is recyclable , contributing to efforts to reduce environmental impact.
EVA copolymers may also be blended with other polymers like LDPE, HDPE, PP, PVC to improve properties such as impact, flexibility.

## Slide 30: INDIAN STANDARDS RELATED TO EVA
IS 13601:1993 -Ethylene Vinyl Acetate (EVA) copolymers for its safe use in contact with foodstuffs, pharmaceuticals and drinking water.
The scope of standard covers the requirements and methods of sampling and test of Ethylene vinyl acetate ( EVA ) copolymer for the manufacture of plastic items used in contact with foodstuffs, pharmaceuticals and drinking water.
The Standard covers various requirements such as Vinyl Acetate Content, Over all migration, Pigments and Colourants. As defined in the Standard IS 13601:1993 the VA content in the EVA Co polymer shall be between 3 % to 50 %. Test method is described in the Annex-B of IS 13601:1993.

## Slide 31: RELATED INDIAN STANDARD 13601:1993

## Slide 32: Applications and Uses
EVA is also used as padding in various equipment ski boots, hockey pads, water ski boots, shoes. EVA is popularly used in slipper and sandals being light weight and cheaper than natural rubber.
Due to its buoyancy , EVA finds it use in floating eye wear.
It is useful in Packaging Industry.
Interlocking tiles
EVA Foam Sheets EVA CROCS made from EVA foam.

## Slide 33: SILICONE RUBBER
Silicone rubber is based on polymeric chains featuring the very stable, alternating combination of silicon (Si) and oxygen (o) atoms in the backbone and a variety of organic side group.
All Silicone rubber have predominantly methyl side groups -CH3

## Slide 34: PROPERTIES OF SILICONE RUBBER
The Silicon rubber have very low glass transition temperatures.
Very high temperature resistance.
Low temperature flexibility
Good Electrical resistance.

## Slide 35: SILICONE APPLICATION Silicon rubber is widely used in industry due to resistant to extreme temperatures (-55 ˚C TO 300 ˚C )

## Slide 36: THERMOPLASTIC ELASTOMER (TPE)
They are class of copolymer or a physical mix of polymers ( usually a plastic and a rubber) which consist of materials with both thermoplastic and elastomeric properties.
Thermoplastic elastomers are processed using a variety of plastic manufacturing equipment such as, injection molding, extrusion, and blow molding. The benefit of using thermoplastic elastomers is the ability to stretch to moderate elongations and return to its near original shape creating a longer life and better physical range than other materials.

## Slide 37: PROCESSING OF THERMOPLASTIC ELASTOMER
Injection molding, extrusion, and
blow molding, are used to
process thermoplastic
Elastomers.

## Slide 38: THERMOPLASTIC ELASTOMER (TPE)
The principal difference between thermoset elastomers and thermoplastic elastomers is the type of cross-linking bond in their structures. In fact, crosslinking is a critical structural factor which imparts high elastic properties.
In order to qualify as a thermoplastic elastomer, a material must have these three essential characteristics:
a) The ability to be stretched to moderate elongations and, upon the removal of stress, return to something close to its original shape.
b) Processable as a melt at elevated temperature.
c) Absence of significant creep.

## Slide 39: PROPERTIES OF TPE
High Elastic Properties.
Thermoplastic elastomer polymers is a weaker dipole or hydrogen bonded.
High molecular weight.
High strength due to vulcanization.

## Slide 40: APPLICATIONS OF TPE
TPE is commonly used to make suspension bushing for automotive performance applications because of its greater resistance to deformation when compared to regular rubber bushings.
Used in Electric Cable Insulation.
Used in adhesive, paints (e.g car coatings).

## Slide 41: ADVANTAGES OF TPE
Elasticity: TPEs have good elasticity and flexibility, which allows them to return to their original shape after being stretched or compressed.
Tensile strength: TPEs have good tensile strength, meaning they can resist being stretched or pulled apart.
Durability: TPEs are resistant to wear and tear, making them suitable for applications where parts are subjected to frequent stress.
Chemical resistance: TPEs can be formulated to have varying levels of chemical resistance, making them suitable for use in a variety of environments.
Temperature resistance: TPEs can be formulated to have varying levels of temperature resistance, with some TPEs suitable for use in high-temperature applications and others suitable for low-temperature applications.
UV resistance: TPEs can be formulated to have varying levels of UV resistance, with some TPEs suitable for outdoor applications and others better suited for indoor applications.
Surface finish: TPEs can have a variety of surface finishes, ranging from glossy to matte.
Recyclability: TPEs can be melted down and re-processed into new parts, making them a more environmentally friendly option than some other materials.

## Slide 42: DISADVANTAGES OF TPE
Thermoplastic elastomers (TPEs) have some disadvantages as well:
Durability under high temperature: TPEs may have limited heat resistance compared to other materials, such as polypropylene or polycarbonate.
Chemical resistance: TPEs are susceptible to degradation by certain chemicals, such as solvents and oils, which can reduce their lifespan.
Surface finish: TPEs may not have the same high-quality surface finish as other materials, such as polycarbonate or acrylonitrile butadiene styrene (ABS), making them unsuitable for certain applications where appearance is important.
Tear strength: TPEs have lower tear strength compared to other materials, making them unsuitable for applications that require high resistance to tearing.
Cost: Depending on the specific application, TPEs may be more expensive than other materials, such as polyethylene or polyvinyl chloride (PVC).
Part warping: TPEs are more prone to warping during the molding process compared to other materials, so they need more precise molding conditions to produce consistent, high-quality parts.

## Slide 43: GUIDELINES ON STORAGE OF RUBBER PRODUCTS AS PER IS 6713:2016
It classifies the rubber products in terms of susceptibility to deterioration of rubber type used.
GROUP A -Rubbers with moderate susceptibility to deterioration by ageing. E.g Butadiene, Isoprene Natural & Synthetic, SBR
GROUP B - Rubbers with low susceptibility to deterioration by ageing. E.g Acrylonitrile Butadiene, Chloroprene rubber,
GROUP C - Rubbers which are highly resistant to deterioration by ageing. E.g Silicone rubber

## Slide 44
RELEVANT
INDIAN STANDARD

## Slide 45: GUIDELINES ON STORAGE OF RUBBER PRODUCTS AS PER IS 6713:2016
Many rubber products and components are stored for long periods before being put in service and thus it is important that they are stored in conditions that minimize unwanted changes in properties. Such changes may occur from degradation which may include excessive hardening, cracking , softening and surface effects.
It is recognized that some rubbers are more susceptible than others to deterioration by such factors as heat, light, ozone, oxygen and humidity. Exposure to these factors should therefore be minimized in order to extend storage life, and to do so a system of storage control, proper packaging and periodic inspection becomes necessary

## Slide 46: REFERENCES
IS 17138 : 2019 Thermoplastic elastomers - Nomenclature and abbreviated terms
IS 6713 : 2016 Rubber products - Guidelines for storage (Second Revision)
IS 3400:Part 1 :2021 Methods of Test for Vulcanized Rubber Part1 Tensile Stress Strain Properties)
IS 3400 (Part 3):2021 Methods of Test for Vulcanized Rubbers Part 3 Abrasion Resistance using a Rotating Cylindrical Drum Device.
IS 3400 (Part 5):2020 Methods of test for rubber, vulcanized or Thermoplastics Part 5 Adhesion of Rubber to Textile Fabrics
IS 3400 (Part 27) : 2019 Methods of test for vulcanized rubbers: Part 27 resistance to ozone cracking - Reference and alternative methods for determining the ozone concentration in laboratory test chambers.
IS 10016 (Part 1) : 1981 Methods of test for polybutadiene rubbers: Part 1 method of taking out test portions from sample bales.
IS 13867:2021 Rubber - General Procedures for Preparing and Conditioning Test Pieces for Physical Test Methods (First Revision)
IS 13601:1993 -Ethylene Vinyl Acetate (EVA) copolymers for its safe use in contact with foodstuffs, pharmaceuticals and drinking water.
IS 5599: 1999- Methods of Sampling and preparation of Rubber –Raw, Natural and Synthetic

## Slide 47: ACCESS TO INDIAN STANDARD